SECTION 03 3053

MISCELLANEOUS CAST-IN-PLACE CONCRETE

*************************************************************************************************************LANL MASTER SPECIFICATION SECTION

Word file at https://engstandards.lanl.gov/specs.shtml

Rev. 11 Summary of Changes Tephra pozzolan-based pre-approved mix designs for NMDOT (Class A, AA, and F) added.

This Section is for unreinforced concrete, thus non-structural.  If it is only being used for a non-code reinforced slab (e.g., certain utility or infrastructure purposes), testing and inspection requirements may be deleted when not desired (there are already provisions for this for a small placement).

For reinforced concrete, use Section 03 3001.

This template must be edited for each project.  In doing so, specifier must add job-specific requirements. Brackets are used in the text to indicate designer choices or locations where text must be supplied by the designer. Once the choice is made or text supplied, remove the brackets. Document must also be edited to delete requirements for processes, items, or designs that are not included in the project -- and specifier’s notes such as these. To seek a deviation from requirements that are applicable, contact the Engineering Standards Manual Civil POC. Please contact POC with suggestions for improvement as well.

When assembling a specification package, include applicable sections from all Divisions, especially Division 1, General requirements.

Section developed for ML-4 projects.  For ML-1, 2, and 3 applications, additional requirements and independent reviews should be added if increased confidence in procurement or execution is desired; see ESM Ch 1 Section Z10 Specifications and Quality sections.
*************************************************************************************************************

GENERAL

*************************************************************************************************************

NOTE: This section may be adjusted to cover separate curbs and gutters or combination curbs and gutters.  This document must not be used for integral or monolithic curbs of concrete pavement.

*************************************************************************************************************

SECTION INCLUDES UNREINFORCED CONCRETE FOR

Sidewalks, drive pads, and median pavement.

Curbs and gutters.

Post- and pole-setting when 8 feet in height or less.

Thrust blocks on utility lines.

Foundations or bases for manholes in non-vehicle-traffic-bearing areas, valve boxes, and test box collars.

ACTION SUBMITTALS

Submit the following:

Material certifications documenting compliance with the New Mexico Department of Transportation (NMDOT) Standard Specifications for Highway and Bridge Construction (SSHBC) including any Supplemental or Interim Specifications (i.e., latest specs).  Exclude NMDOT Division 100, General Provisions, and any other references to METHOD OF MEASUREMENT, to BASIS OF PAYMENT, and for pay factor determination.  Guidance:  Standards Specifications and Drawings

Design mix of each class of concrete, unless LANL pre-approved mix design is used.

Laboratory test reports for design mix for concrete, unless pre-approved mix design is used.

Batch tickets.

Test reports of concrete field testing (except per 3.4.E)

RELATED SECTIONS

Section 31 2000, Earth Moving

Section 03 3001, Reinforced Concrete

Section 01 8113 [LEED v4 and] Guiding Principles 2020: Requirements for water efficiency, energy efficiency, material composition, and indoor air quality requirements.

QUALITY ASSURANCE

Perform work, materials, and construction requirements, in accordance with the NMDOT SSHBC, Section 608, Sidewalks, Drive Pads, and Concrete Median Pavement and NMDOT SSHBC Section 609, Curb and Gutter.

Furnish and place concrete in conformance to the NMDOT Supplemental SSHBC Section 510.

JOB CONDITIONS

Do not place concrete when base surface temperature is less than 40 degrees F.

Perform concrete washout, trucks, and mixers, in a designated and controlled area to prevent the runoff of washout material and the co-mingling of unset concrete with storm water.  Properly dispose of all hardened concrete.

PRODUCTS

  - MATERIALS

Provide materials and construction requirements for forms, concrete, joints, and required accessories conforming to NMDOT SSHBC Section 608, Sidewalks, Drive Pads, and Concrete Median Pavement and NMDOT SSHBC Section 609, Curb and Gutter.

ACCESSORIES

Joint Fillers:  Preformed and meet AASHTO M33 or M153.

  - CONCRETE MATERIALS

    - Cement: ASTM C 150, Type I or Type II.

    - Fine and Coarse Aggregates: Per ASTM C 33.

    - Water: Potable.

    - Pozzolan: Per ASTM C618

  - ADMIXTURES

    - Air Entrainment: Per ASTM C260.

    - Water reduction and Setting Time Modification: Per ASTM C494.

  - CONCRETE MIX

    - Standard Mix Design

      - The standard mix design shall contain from 22–30% (by weight of total cementitious material) Class N pozzolan per ASTM C 618 for mitigating the deleterious effects of ASR in concrete that is common with the siliceous nature of aggregates found in Northern New Mexico. (The pre-approved LATM mixes meet this standard mix design).

    - Provide concrete meeting the following criteria:

      - Exterior Concrete Exposed to Freezing and Thawing:

        - Minimum compressive strength, f ’ c : [4,000 psi @ 28 days].

        - Maximum nominal aggregate size: [0.75 in.]

        - Maximum water / cement ratio: [0.45]

        - Slump: [5 inch]

        - Air content: [6] percent.

      - Exterior Concrete to be Pumped, Exposed to Freezing and Thawing:

        - Minimum compressive strength, f ’ c : [4,000 psi @ 28 days].

        - Maximum nominal aggregate size: [0.75 in.]

        - Maximum water / cement ratio: [0.38].

        - Slump: [6 inch] at discharge of truck.

        - Slump: [3 to 7 ½ inch] at pump discharge.

        - Air content: [6] percent.

      - Interior, not exposed to freezing:

        - Compressive strength, f’ c : [4,000 psi at 28 days].

        - Maximum nominal aggregate size: [0.75 inch].

        - Maximum water/cement ratio: [0.44].

        - Slump: [5 inch.]

        - Air content: [3] percent.

Pre-approved LATM Design Mixes.  These mix designs can be used if material properties remain constant (LANL will verify this periodically).  See Table 1 for detail.

Table 1: LANL Pre-approved LATM Mixes for Miscellaneous Concrete

|  | Exterior Mixes(1) | Interior Mix(1) |
| --- | --- | --- |
| Concrete Design Mix (LATM Mix)(6) | 4K | 4KX (HW) | 4K+ (CW) | CLASS A(7) | CLASS AA(8) | CLASS F(9) | 4KI |
| CA2T (C) or NMDOT Lab Log | C22-149 | C22-149 | C22-149 | 2200-0477 | 2200-0476 | 2200-0488 | C22-150 |
| Concrete Strength (psi) @ 28 days | 4000 | 4000 | 4000 | 3000 | 4000 | 3000 | 4000 |
| Cement - GCC Tijeras I/II (lbs) | 477 | 477 | 477 | 462 | 524 | 447 | 485 |
| Pozzolan - CRM Tephra-NP Class N (lbs) | 143 | 143 | 143 | 138 | 156 | 133 | 145 |
| Coarse Aggregate - El Guique #67 (lbs) | 1816 | 1816 | 1816 | 1847 | 1876 | 1825 | 1873 |
| Fine Aggregate - El Guique Sand (lbs) | 1113 | 1113 | 1113 | 1132 | 1010 | 1216 | 1148 |
| Water (lbs) | 271 | 271 | 271 | 250 | 258 | 233 | 283 |
| Air Content (%)(2) | 6 ± 1.5 | 6.5 ± 1 | 6.5 ± 1 | 6.5 ± 1 | 5.5 ± 1 | 6 ± 1 | 3 ± 1 |
| Air Entraining Admixture(3) (oz/yd3) BASF MasterAir AE200 | 3 – 37 | 3 – 37 | 3 – 37 | 6.0 | 8.8 | 11.6 | – |
| Mid Range Water Reducer(3) (oz/yd3) BASF Polyheed 997 | 19 – 56 | 19 – 56 | 19 – 56 | 30 | 61.2 | 17.4 | 19 -56 |
| Full Range Water Reducer(3) (oz/yd3) BASF Glenium 3030 | 0 – 155 | 0 – 155 | 0 – 155 | – | – | – | 0 – 155 |
| Hydration Stabilizer(3)(4) (oz/yd3) BASF Delvo | – | 24 – 62 | – | – | – | – | – |
| Accelerator(3) (oz/yd3) BASF AC 534 (Formerly NC534) | – | – | 62 – 186 | – | – | – | – |
| Cementitious materials (lbs) | 620 | 620 | 620 | 600 | 680 | 580 | 630 |
| Slump, target (in) | 5 ± 1 | 5 ± 1 | 5 ± 1 | 3.5 ± 1 | 3.5 ± 1 | 1.5 ± 1 | 5 ± 1 |
| Pozzolan (%) | 23 | 23 | 23 | 23 | 22.9 | 22.9 | 23 |
| Water/cementitious ratio (max) | 0.44 | 0.44 | 0.44 | 0.42 | 0.38 | 0.40 | 0.45 |
| Aggregate correction factor | 0.4 | 0.4 | 0.4 | 0.4 | 0.4 | 0.3 | 0.4 |

Table Notes

(1) KX mixes (X = eXtended) provide delayed placement/set, e.g., for hot weather (HW). K+ mixes are for cold weather (CW).

(2) Blistering may occur for mixes with air content higher than 3% if steel trowel finishing is specified.

(3) Admixture quantity range allows for varying dosage based on temperature

(4) BASF MasterSet Delvo added at 4-7 oz/cwt will add an additional 45 minutes of mixing time above the standard 90 minutes. A rate of 7-10 oz/cwt will add an additional 1.5 hours of mixing time above the standard 90 minutes.

(5) note not used

(6) Pre-approved mixes are ‘pumpable’ mixes.

(7) NMDOT Class A: Use for cast-in-place sidewalks, curb/gutter, and concrete wall barrier; other uses by Civil Standards POC permission.  Class AA can be substituted for Class A, but not vice versa.

(8) NMDOT Class AA:  Use for cast-in-place approach slabs and abutments; other uses by Civil Standards POC permission.  Class AA can be substituted for Class A, but not vice versa.

(9) NMDOT Class F:  Use for slip-form-placed wall barrier and curb/gutter; other uses by Civil Standards POC permission.

For work other than DOT usage direction above, use a temperature-suitable suitable 4K mix.

EXECUTION

  - INSPECTION

Verify compacted, treated base is ready to support concrete and imposed loads.

Verify grades and elevations of base are correct.

Verify forms are set to the required grade and alignment and extend to the required depth.

PLACING CONCRETE

Notify the LANL Subcontract Technical Representative (STR) a minimum of 48 hours prior to commencement of concreting operations.

Remove standing water from place of deposit before placement unless permission to do otherwise by LANL.

Ensure that reinforcement, inserts, embedded parts, fence posts, formed joint fillers, joint devices, and formwork are not disturbed during placement.

Place concrete in the forms in one layer.  Consolidate with an approved vibrator.  Finish surface to grade with a strike off.

Install joint fillers, primer, and sealant per manufacturer’s instructions.

Install joint devices per manufacturer’s instructions.

Place concrete continuously between predetermined expansion, control, and construction joints.

Do not use concrete that has been contaminated or has lost its initial workability to the extent that it can no longer be consolidated by the intended method(s).

Concrete Finishing

The surface shall be finished true to grade and section with a wood float or Darby to a smooth and uniformly fine granular or sandy texture free of waves, irregularities, or tool marks.  Sidewalks shall receive a scored surface produced by brooming with a fiber-bristle brush in a direction transverse to that of the traffic, followed by edging.

All slab and sidewalk edges, including those at formed joints, shall be finished with an edger having a radius of 1/4 inch.

Finished concrete slab surfaces shall be free from irregularities.  Check and ensure that the slab has the proper crown, slope, and/or grade.  Trueness shall not vary more than 1/4 inch from the testing edge of a 10-foot straightedge.

Finished concrete sidewalks and curb and gutters shall be free from irregularities.  Check and ensure that the sidewalks, curb and gutters, and medians have the proper crown, slope, and/or grade.  Do not allow the surface of concrete sidewalks, curb and gutters, and medians to deviate more than 1/4 inch (in any direction), if tested with a ten (10) foot straightedge.

Slope top of concrete fence post bases to provide positive drainage.

Finish thrust blocks to the extent where surface voids are eliminated.

CurING AND PROTECTION

    - Immediately after placement, protect concrete from premature drying, excessively hot or cold temperatures and mechanical injury.

    - Cold Weather Concreting

      - Provide adequate equipment for heating concrete materials and protecting concrete during freezing or near-freezing weather.

      - Frozen materials or materials containing ice shall not be used.

      - Forms, fillers, and ground which concrete will contact shall be free from frost and ice.

    - Select concrete materials and production methods so that the concrete temperature at delivery complies with the specified and/or indicated temperature limits.

FIELD QUALITY CONTROL

Provide a certified testing agency to perform field-testing per ACI 301.

Testing agencies performing testing services on concrete materials shall meet the requirements of ASTM C 1077.  LANL Building Official must approve test agency; click for listing of pre-approved agencies.

Field-testing:  By ACI Certified Concrete Field Testing Technician – Grade I, minimum.

Notify the LANL STR 48 hours in advance of field testing to allow for witnessing.

The testing agency shall perform the following tests and collect strength cylinders on one batch in every 50 cu. yards of concrete placed or once a day when less than 50 cu. yards is placed.

Record temperature of concrete per ASTM C 1064.

Perform slump test per ASTM C 143.

Perform air content test per ASTM C 231, pressure method.

Take 4 concrete strength test cylinders per ASTM C 31.

The testing agency shall test the strength test cylinders per ASTM C 39 at 7 days and 28 days.

Concrete to be used for nonstructural purposes that comprises a total quantity of less than 2 cu. yds. (i.e., per project) does not require field testing provided the concrete is mixed per manufacturer’s instructions or approved mix design parameters as reflected by the mix ticket.  For the purposes of this testing exclusion, "nonstructural" will be taken to mean concrete on or below the ground surface that will not adversely affect life safety and does not require a structural design.  Examples of such concrete that meet this definition of nonstructural include sidewalks, curbs, and gutters, thrust blocks, valve boxes, and test box collars, post- and pole-setting when 8 feet in height or less, and manhole collars in non-vehicle-traffic-bearing areas.

DEFECTIVE CONCRETE

Defective concrete is concrete not conforming to strength requirements, not being free from excessive cracking, discoloration, form marks, tool marks, honeycombs, embedded debris, or otherwise non-consistent with the overall appearances of the work.

Do not accept or place defective concrete that is not in conformance with acceptance criteria.  Return the fresh concrete to the supplier.

Replace defective concrete not meeting appearance criteria, at Subcontractor’s expense.  The STR may allow repair of defective concrete at Subcontractor’s expense.

Replace concrete not in conformance with details, tolerances, and other construction requirements at Subcontractor’s expense.

END OF SECTION

************************************************************

Do not delete the following reference information:

************************************************************

THE FOLLOWING STATEMENT IS FOR LANL USE ONLY

This project specification section is based on LANL Master Specification Section 03 3053 Rev. 11, dated May 4, 2023.