SECTION 07 5316

Chlorosulfonate-Polythylene ROOFING

*************************************************************************************************************

LANL MASTER SPECIFICATION

This template must be edited for each project.  In doing so, specifier must add job-specific requirements.  Brackets are used in the text to indicate designer choices or locations where text must be supplied by the designer.  Once the choice is made or text supplied, remove the brackets.  The specifications must also be edited to delete specification requirements for processes, items, or designs that are not included in the project -- and specifier’s notes such as these.  To seek a variance from requirements in the specifications that are applicable, contact the Engineering Standards Manual Architectural POC. Please contact POC with suggestions for improvement as well.

When assembling a specification package, include applicable specifications from all Divisions, especially Division 1, General requirements.

Specification developed for ML-4 projects.  For ML-1, 2, and 3 applications, additional requirements and independent reviews should be added if increased confidence in procurement or execution is desired; see ESM Chapter 1 Section Z10 Specifications and Quality sections.
*************************************************************************************

general

Section includes

Adhered membrane roofing system.

Related sections

    - Comply with Section 07 5050, Membrane Roofing General Provisions.

PRODUCTS

  - PRODUCT OPTIONS AND SUBSTITUTION

    - Alternate products may be accepted; follow Section 01 2500, Substitution Procedures.

acceptable MANUFACTURERS of MEMBRANE MATERIAL

A.	Tremco, Inc.

    - Burkline Industries.

MEMBRANE AND ASSOCIATED MATERIALS

Provide "Hypalon" synthetic rubber as produced by E.I. DuPont de Nemours & Company, formed into uniform flexible sheets, complying with the following:

Also defined as “CSPE”, comprised of a polyester scrim reinforced chlorosulfonated polyethylene (CSPE) sheet, conforming to the following minimum physical properties.

| Property | ASTM Test Method | Specification |
| --- | --- | --- |
| Color |  | Low emissivity, light color (e.g., white) |
| Weight | D751 | 0.29 lb/ft2 |
| Nominal Thickness (min.) | D751 | 0.045 inch |
| Tolerance Thickness (min.) | D751 | + 10 % |
| Breaking Strength (min.) | D751 (Grab Method) | 225 lbf |
| Elongation (min.) | D751 | 25 % |
| Tear Resistance (min.) | D751 (Tongue Method) | 90 lbf (400 N) |
| Ozone Resistance (min.) | D1149 | Pass |
| Low Temperature Flexibility | D2136 | Pass |
| Heat Aging | D573 | Maintains 100 % of Breaking Strength |
| Volatility, Max Loss | D1203, Method A | 0.5 % |
| Hydrostatic Resistance | D751, Method A | 300 psi (2.1 Mpa) |
| Shore A Hardness | D2240 | 80 + 5 |
| Puncture Resistance | FTM 101B, Method 2031 | 200 lbf (900 N) |
| Dimensional Stability (max.) | D1204 | 0.1 % |
| Emmaqua Concentrated Natural Sunlight, 3 million Langleys | E838 | No visible surface cracking or stiffening |

ADHESIVE MATERIALS

Membrane Adhesives: As specified by membrane manufacturer.

Thinner and Cleaner: As specified by adhesive manufacturer, compatible with sheet membrane.

BOARD INSULATION And separation board

Comply with Section 07 2113, Board Insulation.

As approved by membrane manufacturer.

FLASHING

Comply with Section 07 6200, Sheet Metal Flashing and Trim.

Flexible Flashings: Same material as membrane as supplied by manufacturer, thermally welded per manufacturers requirements.

Flashing membrane furnished by roofing membrane manufacturer.  Flashing membranes are generally same materials as roofing membrane unless otherwise specified in Subcontract documents.

ACCESSORIES

Flashing Adhesive: As specified by membrane manufacturer.  Limit adhesives containing carcinogens to vertical surfaces and flashings.

Walktread Membrane: Membrane manufacturer's walktread material.

Wood Nailers: Install treated wood nailers at perimeter of entire roof and around such other roof projections and penetrations as specified in Subcontract documents.  Wood must be #2 or better, treated fire retardant lumber.  Creosote and asphaltic preservatives are prohibited.  Height of nailers must match insulation thickness or as indicated on drawings.  Firmly anchor nailers at maximum spacing of 12 inches unless noted otherwise on drawings and capable of resisting a force of 300 pounds per lineal foot in any direction.  Provide ½-inch expansion spaces between lengths of nailers.

Sealers: As recommended by membrane manufacturer and in compliance with Section 07 9200, Joint Sealers.

Miscellaneous Fasteners and Anchors: In general, all fasteners, anchors, nails and straps must be of zinc-coated steel, galvanized, or stainless steel and cadmium-free.  All fasteners and anchors must have minimum embedment of 1-1/2 inch and must be approved for such use by fastener manufacturer and membrane manufacturer.

Sheet Metal Accessory Materials: ASTM A653, 0.20 percent copper, G90 hot-dipped galvanized, 24 gage or heavier.

Expansion Joint Covers: As specified or as required by membrane manufacturer.

Perimeter Edge Metal: As authorized by membrane manufacturer with minimum 24 gage metal meeting criteria of Section 07 6200, Sheet Metal Flashing and Trim.  Coating to be same material as roofing membrane and compatible with roofing membrane for hot air welding.

Slip-Sheet: Provide only when needed between incompatible materials.  Use membrane manufacturers standard slip-sheet material.

Base Sheet: Provide membrane manufacturers recommended vented base sheet on concrete decks when specified in Subcontract documents or when recommended by membrane manufacturer.

Vapor Barrier: Provide membrane manufacturers recommended Kraft paper vapor barrier between metal decks and insulation when specified in Subcontract documents or when recommended by membrane manufacturer.

EXECUTion

  - INSTALLATION of BOARD INSULATION and separation board

- Comply with Section 07 2113, Board Insulation.

INSTALLATION OF HEAT WELDED SYSTEMS

For heat welded systems, weld adjacent sheets in accordance with manufacturer’s written instructions.  Hot air-weld side and end lap joints.  Lap area must be minimum of 3 inches wide when machine welding, and minimum of 4 inches wide when hand welding.  No adhesive shall be present within lap areas.

Provide hand and machine welding per manufacturer's written instructions.  Workers using welding equipment must have successfully completed a course of instruction provided by a manufacturer's representative prior to welding.  Use welding equipment approved by manufacturer.

Check completed seams after cooling for continuity using a screwdriver or suitable blunt instrument.  In addition, make on-site evaluation of welded seams at locations as directed by the LANL Subcontract Technical Representative (STR) or membrane manufacturer's representative. Provide 2-inch-wide cross-sectional samples taken through completed seams.  Take approximately 2 samples per 100 roofing squares.  When tested correctly, welded seams display failure from shearing of the membrane prior to separation of weld.  Patch each test cut at no additional charge.

Hot air-weld exposed or cured membrane per manufacturer's instructions.

Keep roof area clear of loose or spilled fasteners and metal scraps to guard against accidental roof puncture.

INSTALLATION OF MEMBRANE FLASHING

A.	Install flashing concurrently with roof membrane as job progresses.  Do not use temporary membrane flashing without prior written approval of the LANL STR.  Approval will only be for specific locations on specific dates.

    - Fully adhere flashing membranes to substrates.  Cut and hot air weld interior and exterior corners and miters in place for heat welded systems, or use prefabricated corners and miters.

Bituminous elements must not be in contact with non-compatible membrane flashing.  Use manufacturer’s recommended isolator to isolate non-compatible membrane flashing from bituminous-coated elements such as vent stacks and pipes penetrating the roof.

Flashing for hot welded systems must be hot-air welded at their joints and at their connections with roof membrane.

Flash pipe penetrations minimum 8 inches above roofing membrane, and terminate with stainless steel hose clamp with sealant applied along top edge.  Pipe must be isolated with membrane flashing.  Factory fabricated pipe seals and roof membrane must be specified by membrane manufacturer.  Install a buffer layer of membrane between hose clamp and flashing sheet to avoid damage.

Mechanically fasten curb flashing membranes along top using nails with 1 inch diameter heads spaced maximum 6 inches on center, or use predrilled metal strips.  Caulk predrilled metal strips along top edge with sealant.  Use expansion pins with nylon sheaths set in predrilled holes to secure flashing to masonry and concrete surfaces. Use reglets on walls as shown in Subcontract documents.

Provide edge metal approved by membrane manufacturer.

END OF SECTION

******************************************************************

Do not delete the following reference information:

******************************************************************

FOR LANL USE ONLY

This project specification is based on LANL Master Specification 07 5316 Rev. 1, dated May 5, 2008.